CERTIFICATE  OF  ANALYSIS

| Product Name | Trihydroxystearin | Specification | Company Standard |
| --- | --- | --- | --- |
| Cas No. | 139-44-6 | Manufacture Date | 2024.1.22 |
| Quantity | 100KG | Analysis Date | 2024.1.28 |
| Batch No. | BF-240122 | Expiry Date | 2026.1.21 |
| Items | Specifications | Results |
| Acid Value(ASTM D 974),KOH/g | 0-3.0 | 0.9 |
| Heavy Metals,%(ICP-MS) | 0.00-0.001 | 0.001 |
| Hydroxyl Value, ASTM D 1957 | 154-170 | 157.2 |
| Iodine Value, Wijs Method | 0-5.0 | 2.5 |
| Melting Point(℃) | 85-88 | 86 |
| Saponification Value (Potassium hydroxide method) | 176-182 | 181.08 |
| +325 Mesh Residue % (Retain) | 0-1.0 | 0.3 |

Conclusion: Approved                                                  Tested by: Zhang Xiaoxuan