CERTIFICATE  OF  ANALYSIS

| Product Name | Sodium Stearate | Specification | Company Standard |
| --- | --- | --- | --- |
| Cas No. | 822-16-2 | Manufacture Date | 2024.2.17 |
| Quantity | 100KG | Analysis Date | 2024.2.23 |
| Batch No. | BF-240217 | Expiry Date | 2026.2.16 |
| Items | Specifications | Results |
| Appearance@25℃ | Free Flowing Powder | Pass |
| Free Fatty Acid | 0.2-1.3 | 0.8 |
| Moisture % | 3.0 Maximum | 2.6 |
| C14 Myristic % | 3.0 Maximum | 0.2 |
| C16 Palmitic % | 23.0-30.0 | 26.6 |
| C18 Stearic % | 30.0-40.0 | 36.7 |
| C20+C22 | 30.0-42.0 | 36.8 |
| Heavy Metals,ppm | 20 Maximum | Pass |
| Arsenic,ppm | 2.0 Maximum | Pass |
| Microbiological Count, cfu/g (total plate count) | 10 (2) Maximum | Pass |

Conclusion: Approved                                                  Tested by: Zhang Xiaoxuan