CERTIFICATE  OF  ANALYSIS

| Product Name | Carbomer 980 | Manufacture Date | 2024.1.21 |
| --- | --- | --- | --- |
| Quantity | 500KG | Analysis Date | 2024.1.28 |
| Batch No. | BF-240121 | Expiry Date | 2026.1.20 |
| Items | Specifications | Results | Method |
| Appearance | Fluffy, white powder | Complies | visual inspection |
| Viscosity (0.2% Aqueous Solution) mPa · s | 13000 ~30000 | 20500 | rotational viscometer |
| Viscosity (0.5% Aqueous Solution) mPa · s | 40000 ~60000 | 52200 | rotational viscometer |
| Residual Ethyl Acetate / Cyclo hexane % | ≤ 0.45% | 0.43% | GC |
| Residual Acrylic Acid % | ≤ 0.25% | 0.082% | HPLC |
| Transmittance( 0.2 % Aqueous Solution) % | ≥ 85% | 96% | UV |
| Transmittance( 0.5 % Aqueous Solution) % | ≥85% | 94% | UV |
| Loss on Drying % | ≤ 2.0% | 1.2% | Oven method |
| Bulk density g/100mL | 19.5 -23. 5 | 19.9 | tapping apparatus |
| Hg(mg/kg) | ≤ 1 | Complies | Outsourcing inspection |
| As( mg/kg) | ≤ 2 | Complies | Outsourcing inspection |
| Cd(mg/kg) | ≤ 5 | Complies | Outsourcing inspection |
| Pb(mg/kg) | ≤ 10 | Complies | Outsourcing inspection |
| Conclusion | Sample Qualified. |

Conclusion: Approved                                                  Tested by: Zhang Xiaoxuan