CERTIFICATE  OF  ANALYSIS

| Product Name | Lanolin Anhydrous | Manufacture Date | 2024.3.11 |
| --- | --- | --- | --- |
| Quantity | 100KG | Analysis Date | 2024.3.18 |
| Batch No. | BF-240311 | Expiry Date | 2026.3.10 |
| Items | Specifications | Results |
| Appearance | Yellow, half solid ointment | Complies |
| Water-soluble acids & alkalis | Relevant requirements | Complies |
| Acid value (mgKOH/g) | ≤ 1.0 | 0.82 |
| Saponification (mgKOH/g) | 9.-105 | 99.6 |
| Water-soluble oxidizable substance | Relevant requirements | Complies |
| Paraffins | ≤ 1% | Complies |
| Pesticide residues | ≤40ppm | Complies |
| Chlorine | ≤150ppm | Complies |
| Loss on drying | ≤0.5% | 0.18% |
| Sulfated ash | ≤0.15% | 0.08% |
| Drop point | 38-44 | 39 |
| Color by gardner | ≤10 | 8.5 |
| Identification | Relevant requirements | Complies |
| Conclusion | Sample Qualified. |

Conclusion: Approved                                                  Tested by: Zhang Xiaoxuan