CERTIFICATE  OF  ANALYSIS

| Product Name | Myristic Acid Powder | Specification | Company Standard |
| --- | --- | --- | --- |
| Cas No. | 544-63-8 | Manufacture Date | 2024.2.22 |
| Quantity | 100KG | Analysis Date | 2024.2.28 |
| Batch No. | BF-240222 | Expiry Date | 2026.2.21 |
| Items | Specifications | Results |
| Appearance | White Crystalline Powder | Conforms |
| Acid Value | 245.0-255.0 | 245.7 |
| Saponification Value | 246-248 | 246.9 |
| Iodine Value | ≤0.5 | 0.1 |
| Heavy Metals | ≤20 ppm | Conforms |
| Arsenic | ≤2.0 ppm | Conforms |
| Microbiological Count | ≤10 cfg/g | Conforms |
| Conclusion | This sample meets the specifications. |

Conclusion: Approved                                                  Tested by: Zhang Xiaoxuan