CERTIFICATE  OF  ANALYSIS

| Product Name | Rice Bran Wax | Manufacture Date | 2024.2.22 |
| --- | --- | --- | --- |
| Quantity | 500KG | Analysis Date | 2024.2.29 |
| Batch No. | BF-240222 | Expiry Date | 2026.2.21 |
| Examination |
| Items | Specifications | Results |
| Melting Point | 77℃-82℃ | 78.6℃ |
| Saponification Value | 70-95 | 71.9 |
| Acid value (mgKOH/g) | 12Max | 7.9 |
| Lodine value | ≤ 10 | 6.9 |
| Wax content | ≥ 97 | 97.3 |
| Oil content (%) | 0-3 | 2.1 |
| Moisture (%) | 0-1 | 0.3 |
| Impurity (%) | 0-1 | 0.3 |
| Color | Light Yellow | Complies |
| Arsenic (As) | ≤ 3.0ppm | Complies |
| Lead | ≤ 3.0ppm | Complies |
| Conclusion | Sample Qualified. |

Conclusion: Approved                                                  Tested by: Zhang Xiaoxuan