CERTIFICATE  OF  ANALYSIS

| Product Name | Sodium Hyaluronate | MF | (C14H20NO11Na)n |
| --- | --- | --- | --- |
| Cas No. | 9067-32-7 | Manufacture Date | 2024.1.25 |
| Quantity | 500KG | Analysis Date | 2024.1.31 |
| Batch No. | BF-240125 | Expiry Date | 2026.1.24 |
| Items | Specifications | Results |
| Physical Properties | White or almost white powder or granular, odorless, very hygroscopic. Soluble in water to form clarified solution, insoluble in ethanol, acetone or diethyl ether. | Qualified |
| ASSAY |
| Glucuronic Acid | ≥ 44.5% | 46.44% |
| Sodium Hyaluronate | ≥ 92.0% | 95.1% |
| ROUTINE |
| pH (0.5% aq.sol., 25℃) | 6 .0 ~ 8.0 | 7.24 |
| Transmittance (0.5% aq.sol., 25℃) | T550nm ≥ 99.0% | 99.0% |
| Absorbance (0.5% aq. sol., 25℃) | A280nm ≤ 0.25 | 0.23% |
| Loss on Drying | ≤ 10.0% | 4.79% |
| Residue on Ignition | ≤ 13.0% | 7.90% |
| Kinematic Viscosity | Measured Value | 16.84% |
| Molecular Weight | 0.6 ~ 2.0 × 106 Da | 0.6x106 |
| Protein | ≤ 0.05% | 0.03% |
| Heavy Metal | ≤ 20 mg/kg | < 20 mg/kg |
| Hg | ≤ 1.0 mg/kg | < 1.0 mg/kg |
| Pb | ≤ 10.0 mg/kg | < 10.0 mg/kg |
| As | ≤ 2.0 mg/kg | < 2.0 mg/kg |
| Cd | ≤ 5.0 mg/kg | < 5.0 mg/kg |
| MICROBIAL |
| Bacteria Counts | ≤ 100 CFU/g | < 100 CFU/g |
| Molds & Yeasts | ≤ 10 CFU/g | < 10 CFU/g |
| Staphylococcus Aureus | Negative | Negative |
| Pseudomonas Aeruginosa | Negative | Negative |
| Thermotolerant Coliform Bacteria | Negative | Negative |
| Salmonella | Negative | Negative |
| Storage Condition | In an airtight container, protected from light, cold storage 2℃ ~ 10℃ . |
| Package | 10kg/carton with inner 2 layers of PE bag, or 20kg/drum. |
| Conclusion | This sample meets the standard. |

Conclusion: Approved                                                  Tested by: Zhang Xiaoxuan